**Products**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Acrylic All Purpose Primer | Acrylic Matt | Acrylic Low Sheen | Acrylic Satin | Acrylic Gloss |
| Coverage | Up to 20 square metres per litre per coat (varies with substrate and texture) |
| Touch dry & recoat times | Between 20 minutes and 1 hour |
| Scrub resistance | N/A  | Class 1 | Class 1 | Class 1 | Class 1 |
| Marking resistance | N/A | N/A | Good | Excellent | Excellent |
| Cleaning ability | N/A  | Good | Excellent | Excellent | Excellent |
| Adhesion | Excellent | Excellent | Excellent | Excellent | Excellent |
| Flexibility | Good | Good | Excellent | Excellent | Excellent |
| Volatile Organic Compounds (VOCs) | 15g/l | 10g/l | 14g/l | 25g/l | 45g/l |
| VOCs EU 2010 limit | 30g/l | 30g/l | 130g/l | 130g/l | 130g/l |
| Sheen level | N/A | 3% | 7% | 20% | 80% |
| Colour range | White | All colours | All colours | All colours | All colours |
| Pail sizes | 1,2.5 and 5 litre | 5 and 10 litre | 2.5,5 and 10 litre | 1,2.5,5 and 10 litre | 1,2.5 and 5 litre |
| Sanding ability | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Interior | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Exterior | Checkmark | Close | Checkmark | Checkmark | Checkmark |
| Solid plaster | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Fibrous plaster | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Gypsum plaster | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Plasterboard | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Timber | Checkmark | Close | Checkmark | Checkmark | Checkmark |
| MDF | Checkmark | Checkmark | Checkmark | Checkmark | Checkmark |
| Timber cladding | Checkmark | Close | Checkmark | Checkmark | Checkmark |
| Ferrous and non-ferrous metal \* | Close | Close | Close | Checkmark | Checkmark |
| Concrete & brick | Close | Close | Checkmark | Checkmark | Checkmark |
| PVC # | Checkmark | Close | Checkmark | Checkmark | Checkmark |
| Previously painted aged alkyd / oil finishes | Checkmark | Close | Checkmark | Checkmark | Checkmark |

* Apply a proprietary metal primer prior to applying top coat.
* It is essential that plastic surfaces are cleaned and sanded to provide a key, followed by an application of Paintfinity’s Acrylic All Purpose Primer before applying top coats.